## Slide 1: Development Problems for Sail Segments <7.xx µm 1st International Symposium on Solar Sailing 27-29 June 2007 Herrsching, Germany Dr. F. Lura

## Slide 2: Design and Manufacturing of Sail Segments
Design & Procurement
Our baseline for a sail design are 4 triangular sail segments (Fig. 1) .
Some inquiries have been started regarding
the general possibility to procure both side
coated foils less than 7,5 µm.
Main problem seems to be the thermal load
during the vacuum deposited coating process.
Following, in the case of success to get
useable both side coated foils in the 3…4 µm
Fig. 1 Triangular sail segment
range, first manufacturing attempts and the production of a triangular small-scale sail
segment sample with a surface of 9 m2 are planned (restricted by vacuum table size).

## Slide 3
Status available sail film thickness
No PEN or PI – films with thickness < 7,x µm - coated with VDA of required
quality are available up to now!
Reason: Considerable technological problems due to temperature load during the process of metallization and high expense required to develop new special technology
Official statement from DUNMORE Corp./TRICON (dated 07.05.2007)
"we got your inquiry passed on from our US colleagues. It is correctly that we at that time (still as TRICON) 4µm PEN metallized. However with seriously problems by temperature loads of our process. We had holes and outlines in the foils and finally supplied we only one subset of the originally required quantity. We would drive an new attempt only without any warranty and against Maschinenstundenkosten for you. For 2 µm it does not go reliably not."

## Slide 4
Status available sail film thickness
• Expense for an attempt to find a technological solution for manufacturing of high quality foils VDA in the  7 µm range is
in a cost range of 300.000 EURO !! (telephone message TRICON)
• Success is uncertain; to find other companies for high quality foils VDA in the  7 µm range – too
• But 
However: we have to clear other hurdles too on the way to optimum sail foils

## Slide 5: Influence of wrinkles on reflectance
Conclusion: avoid wrinkles

## Slide 6: Influence of coating material on reflectance
Al-typically
To do: optimize the coating

## Slide 7
Enhancement of reflectance due to suitable combination of coatings
(it is reality for smooth optical surfaces)
Find equivalent measures for foils

## Slide 8
Enhancement of reflectance due to suitable combination of coatings
(it is also valid for flexible foils?)
Samples of Kapton 7,5 µm with VDA + 80 nm SiO2 + 57 nm TiO2 coating system, manufactured by ASTRAL (USA) were procured. First measurements were carried out, in order to approve the properties with flexible material before and after handling processes
?

## Slide 9
Enhancement of reflectance due to suitable combination of coatings
(it is not (?) valid for flexible foils)
We have to clarify the reason for the dramatic difference by comparative tests (optical polished glass target versus foil and same vacuum deposition technology).
Possibly the change of the foils roughness could be a effect. It is to investigate by scanning electron microscopy.

## Slide 10: Influence of roughness on reflectance
Take care of smooth foils

## Slide 11: Degradation effects by environmental loads related to the reflectance of sail foils
Our irradiation tests in 2004 with complex radiation (solar radiation, included VUV, electron- and proton radiation) gave us indications for the degradation.
The irradiated foils showed a light brown colouring after the test. But it could be also an indication for self-contamination coming from the test facility
The reflection spectra of the irradiated and unirradiated foil samples were examised with a Lambda 19 spectrophotometer.
The main reduction of the reflection degree reaches values of 2% up to 4 % was found in the maximum range of the spectral irradianz of solar radiation.
These test results are significant to stimulate the discussion again around the real available propulsion force, because almost ideal reflection was past assumption. Realistically probably only appr. 90% in maximum remain, which can be further reduced also more by other degradation effects.

## Slide 12
Irradiation-facility KOBE for degradation investigations
Source | Performance
p+/e- - source | 10 – 100 keV beam; current:0,1 – 100 µA
Solar simulator | up to 3,8 suns; per ASTM E-490
High-power Deuterium | 0,36 W/m2 ; 115-400 nm
VUV- source | 1,5 W/m2; 5 – 180 nm
To remove any traces of self-contamination a new generation of KOBE (KOmplexe BEstrahlungs-Anlage) is in development in the DLR Space System Institute.
The facility enables the complex and simultaneous simulation of the essential space environment factors for the investigation of materials and surfaces for space applications. The complex for the simultaneous and co-directed radiation stress includes